## Slide 1: On Predicting Microstructural Evolution from the Dependence of Phase Gibbs Free Energy on the Thermal Gradient
Prof. Ivaldo Leão Ferreira
Faculty of Mechanical Engineering, Federal University of Pará, UFPA
Augusto Corrêa Avenue 1
66075-110, Belém, PA, Brazil

## Slide 2: Motivation
Our experimental cooling rates range from 2100 to 120 K/min, whereas equilibrium is reached at less than 5 K/min;
The Classical Nucleation Theory (CNT) provides an inadequate description of thermodynamic equilibrium shifts;
The CNT’s core equation – a limiting case for infinite volume – overemphasizes bulk free energy contributions when considering finite surface energies, i.e., ;
The undercooling is dependent on the thermal gradient and surface free-energy changes considerably;
Recent research by Ferreira (2024) and Ferreira et al. (2025) on phase nucleation demonstrates a closed-form parabolic relationship in terms of the nucleation radius.

## Slide 3: OBjectives
Remain in the continuum mechanics scale to easily calculate the surface stress tensor and make DTA/DSC experiments for equilibrium conditions;
Derive a general phase transformation equation within this domain by combining the First and Second Laws of Thermodynamics;
Present a novel formulation of phase nucleation;
Apply fundamental thermodynamic variables and functions to analyze this new field;
Investigate the effects of thermal gradients on free Energies;

## Slide 4: A Proper Field for Phase Transformation
The First Law of Thermodynamics,
This means, . Energy is a point function and, and are path-dependent quantities, i.e., line functions
Let’s then define a new field, by making from tensor calculus, , in relation to primitive variable, we can express the 1st Law of Thermodynamics as

## Slide 5: A Proper Field for Phase Transformation
The thermal field can be defined as:
Path-independent thermal field gradient
Path-dependent thermal field gradient
Thermal-fields relationship gradient

## Slide 6: A Proper Field for Phase Transformation
By considering LHS and RHS, the following expression can be deduced,
By the First Law, , presents and as independent variables, and can be neglacted. Finally, the path-dependent thermal field in [K] can defined as,
and, field derived in 2024 in Ferreira [2024] DOI: 10.1016/j.physb.2024.416494

## Slide 7: A Proper Field for Phase Transformation
The energy can be written in terms of , (Emmy Noether’s SIMMETRY)
By the First Law,
where, can be written as to give ,

## Slide 8: A Novel Phase Nucleation Formulation
The crítical total free energy in Ferreira [2024] DOI: 10.1016/j.physb.2024.416494 can be deduced in terms of the bulk and surface free energies as,
where, . When deriving with respect to the critical radius to determine the maximum of , the following parabolic equation is obtained,

## Slide 9: A Novel Phase Nucleation Formulation
A 2nd-order critical radius can be derived from nucleation formulation in terms of bulk , surface , and configurational free energies as given,
and, the 1st-order approximation of critical radius can be expressed as the following
By comparing with CNT,

## Slide 10: A Novel Phase Nucleation Formulation
A 2nd-order thermal field tensor can be derived by maximum of total Gibbs-free energy,
And 1st-order approximation for the thermal field tensor can be derived as given,
The nucleation rate derived by Ferreira (2024) is given by
where, is the self-diffusion coefficient in , is the density of modes in the new phase in , is the distance an atom must jump from a phase to the nucleating new surface area in m, is the surface area of the new phase in .

## Slide 11: A General Phase Transformation Equation
The newly thermal field Tensor as derived by Ferreira [2024] DOI: 10.1016/j.physb.2024.416494 is defined as any new created and deformed surface area is normal to the termal field , i.e.,
Examples of application,

## Slide 12: Application of Fundamental Thermodynamics Variables and Functions to this New Field
The solution of the thermal field tensor requires:
The solution of the surface-stress tensor [Gurtin and Murdoch, 1978; Ferreira (2022)]
on surface
where , E and u are the stress, the strain and displacement fields.
A metric tensor, in this case, in spherical coordinates, and its contravariant,
, and the initial conditions,

## Slide 13: Application of Fundamental Thermodynamics Variables and Functions to this New Field
The solutionofthethermalfield Tensor requires:
The Surface Free Energy [Ferreira, (2021, 2022, and 2024)]:
Considering a 2-Sphere, the Ricci scalar is ,
where is a dimensionless geometric function; its argument is the only admissible scalar curvature invariant, , , , and are the surface energy in [J.m-2], the radius at the thermodynamic state 0 (assumed as equilibrium or initial condition vector radius for Equilibrium, i.e., ) in [m], the surface stress tensor in [N.m-1], and the Ricci scalar, respectively.

## Slide 14: Application of Fundamental Thermodynamics Variables and Functions to this New Field
The solutionofthethermalfield Tensor requires:
The Surface Entropy [Ferreira, (2021, 2022, and 2024)]:
Considering a 2-Sphere, the Ricci scalar is ,
where , , , and are the surface energy in [J.m-2], the radius at the thermodynamic state 0 (assumed as equilibrium or initial condition vector radius for Equilibrium, i.e., ) in [m], the surface stress tensor in [N.m-1], and the Ricci scalar, respectively.

## Slide 15: Application of Fundamental Thermodynamics Variables and Functions to this New Field
The solutionofthethermalfield Tensor requires:
The Surface Energy Potential [Ferreira, (2021, 2022, and 2024)]:
Considering a 2-Sphere, the Ricci scalar is , since , and
where , , , and are the surface energy in [J.m-2], the radius at the thermodynamic state 0 (assumed as equilibrium or initial condition vector radius for Equilibrium, i.e., ) in [m], the surface stress tensor in [N.m-1], and the Ricci scalar, respectively.

## Slide 16: Application of Fundamental Thermodynamics Variables and Functions to this New Field
The solutionofthethermalfield Tensor requires:
The Surface Entropy Potential [Ferreira, (2021, 2022, and 2024)]:
Considering a 2-Sphere, the Ricci scalaris, since , , and
where , , , and are the surface energy in [J.m-2], the radius at the thermodynamic state 0 (assumed as equilibrium or initial condition vector radius for Equilibrium, i.e., ) in [m], the surface stress tensor in [N.m-1], and the Ricci scalar, respectively.

## Slide 17: Experimental Validation, : SDAS
PDAS
SDAS

## Slide 18: Application Example 1
Experimental validation [Ferreira et al. (2025)]:
SDAS can be calculated in terms of Gibbs-Thomson which is the Thermal Field Tensor as,

## Slide 19: Application Example 1
Experimental validation [Mendes et al. (2023)]:
Figure 1 Schematic representation of transient horizontal solidification experiment.

## Slide 20: Application Example 1
Experimental validation [Mendes et al. (2023)]:
Figure 2 Experimental data from transient solidification measurements yielded (A) dendrite tip growth rates, (B) liquidus thermal gradients, and (C) dendrite tip cooling rates.
( A )

## Slide 21: Application Example 1
Experimental validation [Mendes et al. (2023)]:
Figure 3 Experimental data from transient solidification measurements yielded (A) dendrite tip growth rates, (B) liquidus thermal gradients, and (C) dendrite tip cooling rates.
( B )

## Slide 22: Application Example 1
Experimental validation [Mendes et al. (2023)]:
Figure 4 Experimental data from transient solidification measurements yielded (A) dendrite tip growth rates, (B) liquidus thermal gradients, and (C) dendrite tip cooling rates.
( C )

## Slide 23: Application Example 1
Results of Nucleation Calculation [Present work]:

## Slide 24: Application Example 1
Results of Nucleation Calculation [Present work]:

## Slide 25: Application Example 1
Experimental validation [Present work]:
Figure 5 Thermal field tensor (Gibbs-Thomson) function of thermal gradient.
( A )

## Slide 26: Application Example 1
Experimental validation [Ferreira et al. (2025)]:
SDAS can be calculated in terms of Gibbs-Thomson which is the Thermal Field Tensor as,

## Slide 27: Application Example 1
Experimental validation [Present work]:
Figure 6 Comparison between secondary arm-spacing models and experimental scatter.
( A )

## Slide 28: Application Example 2
Experimental validation [Marques et al. (2025)]:
Figure 15 Experimental data from transient solidification measurements yielded (A) dendrite tip growth rates, (B) liquidus thermal gradients, and (C) dendrite tip cooling rates.
( B )

## Slide 29: Application Example 2
Experimental validation [Marques et al. (2025)]:
Figure 16 Thermal field tensor (Gibbs-Thomson) function of thermal gradient.

## Slide 30: Application Example 2
Experimental validation [Marques et al. (2025)]:
Figure 17 Comparison between secondary arm-spacing models and experimental scatter.
( A )

## Slide 31: Application Example 1
Experimental validation [Ferreira et al. (2025)]:
Figure 7 Gibbs bulk free-energy as a function of thermal gradient.
( A )

## Slide 32: Application Example 1
Experimental validation [Present work]:
Figure 8 Gibbs surface free-energy as a function of thermal gradient.
( A )

## Slide 33: Application Example 1
Experimental validation [Present Work]:
Figure 9 Gibbs configurational free-energy as a function of thermal gradient.
( A )

## Slide 34: Application Example 1
Experimental validation [Present work]:
Figure 10 Bulk entropy as a function of thermal gradient.
( A )

## Slide 35: Application Example 1
Experimental validation [Present work]:
Figure 11 Surface entropy as a function of thermal gradient.
( A )

## Slide 36: Application Example 1
Experimental validation [Present work]:
Figure 12 Configurational entropy as a function of thermal gradient.
( A )

## Slide 37: Application Example 3
Surface Energy Validation [Present work]:
Figure 14 Vapour–liquid interfacial energy along the solved continuation. The full geometric surface-free-energy model (black solid) is compared with the Tolman curvature law (red dashed) over the solved domain (shaded). The two laws coincide in the planar, gradient-free limit and separate as r decreases and increases, the departure measuring the thermal-field coupling of the surface energy that the Tolman law omits. Axes: droplet radius r in m, decimal logarithm of the thermal gradient in , and interfacial energy γ in .

## Slide 38: Conclusions
1. The second-order nucleation formulation, in relation to the critical radius, was validated and experimentally confirmed as a valid scientific theory;
2. The nucleation process analyzed has shown quadratic behavior in terms of nucleation radius;
3. Bulk and configurational free energies exhibit opposing signs relative to surface free energy;
4. Because the substrate’s contribution aims to minimize local free energy, the configurational and bulk free energies share the same sign.

## Slide 39: References
[1] I.L. Ferreira Physica B: Condensed Matter. 695 (2024) 416494.
[2] I.L. Ferreira: Materials. (2026) in press.
[3] Y.-B. Kang, Calphad: Comput. Coupling Ph. Diagr. Thermochem. 50 (2015) 23
[4] L.P. Marques et al. Mater. Res., 28 (2025) e20250045-7.
[5] I.L. Ferreira et al. Mater. Res., 28 (2025) e20250069.

## Slide 40: Thanks for Watching!
Funding: The Authors acknowledge the financial support provided by CAPES (Coordenação de Aperfeiçoamento de Pessoal de Nível Superior - Brazil) Finance Code 001 and Grant 88881.707312/2022-01, and CNPq (National Council for Scientific and Technological Development - Brazil) Grant 301502/2022-6, and FAPESPA (Fundação Amazônia de Amparo a Estudos e Pesquisas).
Special thanks to Project “Energy Recovery from Agricultural and Forestry Waste in the States of Amazonas, Pará, and Mato Grosso: Sustainable Production of HVO, Biogas, Biometane, and Green Hydrogen for Use in Internal Combustion Engines”, CNPq Grant 445608/2024-2.